Contour 300 – Self Contained Breathing Apparatus

Technical Datasheet

Description

The Scott Contour 300 is an open circuit, self-contained, compressed air breathing apparatus. It consists of a back plate, padded carrying harness and pneumatic system, consisting of a cylinder connector, reducer, pressure gauge, whistle and demand valve.

The Contour 300 can be configured in a number of different ways with various size single cylinders.  There are also a range of attachments available including Airline, Split Demand Valve Coupling (SDC),

Rescue Second Man (RSM) and Decontamination.

The Contour 300 is used in conjunction with a range of composite or steel cylinders and the choice of Vision 3, Panaseal, Panavisor or Promask PP facemask.

Applications

The Contour 300 is specifically designed as a Professional/Industrial Fire Fighting SCBA, but is also suitable for providing respiratory protection for any IDLH environment.

Approval Information

1	CE marked in accordance with EN137:1998

2	CE marked in accordance with EN139 – sets fitted with CEN airline attachments

3	AS1716

Materials

| Pressure Reducing Valve | Nickel Plated Brass |
| --- | --- |
| Rust Tube (Sabre Cyls) | Brass |
| Reducing Valve Seat | Polyamide (Nylon) |
| O-Rings | Nitrile, Silicone, EPDM |
| Reducing Valve Springs | Stainless Steel |
| HP Pressure Gauge | Stainless Steel, Polycarbonate Lens |
| HP Pressure Gauge Cover | Neoprene |
| MP Air Supply Hose Fittings | Nickel Plated Brass |
| Facemask | Neoprene, Silicone or Procomp |
| Facemask Visor | Polycarbonate |
| MP Air Supply Hose | Chlorinated Polyethylene, fabric braid reinforcement, Nitrile liner |
| HP Air Hose | PTCFE liner, stainless steel braiding, Estane sleeve |
| Valve Handwheel (Sabre Cyls) | Glass filled Polyamide |
| Harness | Intrinsically flame retardant 50% Kevlar blend webbing and Nomex 3 fabric |
| Backplate | Glass & Carbon filled Nylon composite |
| Backpad | Flame retardant polyamide and closed cell Polyethylene foam |
| Cylinder Band | 100% Kevlar |
| Strap Buckles | Stainless Steel, Brass |
| Cylinder | Steel or Composite |
| Cylinder Valve | Nickel Plated Brass |
| Demand Valve Casing | Glass filled Polyacetal and Polyamide |

Maintenance/Servicing/Cleaning

N.B. - Cleaning should only be carried out as specified in the user instructions.

Maintenance and Servicing must only be performed by trained personnel following the procedures in the Service and Maintenance manual.

Technical Specifications

| Tempest Demand Valve Compact positive pressure demand valve featuring servo-assisted, tilting diaphragm mechanism with low inspiratory resistance and responsive dynamic performance, automatic first breath actuation and hands free bypass facility. Components injection moulded from Polyamide and Acetyl with rubber seals and diaphragms. |  |
| --- | --- |
| First breath activation | -20 to -30 mbar |
| Peak flow performance | In excess of 500 litres/minute |
| Bypass flow | 150 litres/minute nominal |
| Static positive pressure | 1.0 – 4.0 mbar |
| Reducing Valve First stage pressure reducing valve featuring non-adjustable, spring loaded piston mechanism and outlet supply protected by pressure relief valve. Valve body and cap machined from nickel-plated brass with stainless steel spring and hose retainer U-clips. |  |
| Outlet pressure |  |
| 200 bar inlet | 5.5 to 9.5 bar |
| 300 bar inlet | 6.0 to 11.0 bar |
| Pressure relief valve protected | Approx. 13.5 bar |
| Flow restrictor to gauge supply hose | <25 litres minute |
| Pressure Indicator & Warning Whistle Bourdon tube type dial indicator Heat and Impact resistant Polycarbonate lens |  |
| Safety blow-out vent in rear of gauge:- | Accuracy:- +/- 10 bar between 40-300 bar |
| Hoses Stainless steel swivel hose fittings |  |
| Medium pressure hose |  |
| Maximum working pressure | 16 bar |
| Minimum burst pressure | 80 bar |
| High pressure hose |  |
| Maximum working pressure | 450 bar |
| Minimum burst pressure | 800 bar |
| Packing Specifications |  |
| Single | 69x41x28cm 5kg |
| Weight/Dimensions |  |
| Single configuration (less cylinder) | 2.3kg |
| Single configuration & facemask (less cylinder) | 3.0kg |
| Length | 600mm |
| Width | 278mm |
| Depth (with 6.0 litre 200 bar cylinder) | 200mm |